Guth Model

Table xx: Optimized A and B parameters for each data set and the corresponding mean absolute percentage error (MAPE) for each material. “Averaged” refers to the mean performance of individually optimized parameters for each material, while “All materials combined” indicates the results obtained by optimizing parameters using a data set that includes all three materials collectively.

| Optimizer | A | B | FM | Cerr 117 | Cerr 158 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| FM | 2.7845 | 0.6413 | 7.6 | 10.85 | 15.75 | 11.4 |
| Cerr 117 | 2.9741 | 0.2879 | 11.77 | 5.77 | 10.29 | 9.28 |
| Cerr 158 | 3.1184 | 0.0727 | 14.65 | 7.68 | 8.85 | 10.39 |
| Averaged | 2.959 | 0.3339 | 11.09 | 5.86 | 10.98 | 9.31 |
| All materials combined | 3.0462 | 0.1803 | 13.21 | 6.72 | 9.1 | 9.68 |
| Buckner et al | 0.67 | 1.62 | 16.42 | 18 | 18.6 | 17.67 |
| Guth | 2.5 | 14.1 | 378.19 | 409.48 | 440.17 | 409.28 |

Final selected values A =3 and B = 0.3

Trust-Region-Reflective Algorithm

| Model | Filler Type | Equation Form | Best For | Limitations | Citation / Origin |
| --- | --- | --- | --- | --- | --- |
| Guth–Gold | Spherical | Ec=Em(1+2.5ϕ+14.1ϕ2)E_c = E_m (1 + 2.5\phi + 14.1\phi^2) | Rubber with spherical fillers (e.g., silica, carbon black) | Limited to low filler fractions, assumes perfect dispersion | Guth & Gold, Phys. Rev. 1945 |
| Kerner Model | Spherical | Analytical (complex) | Thermoplastics and rubbers with spherical particles | Assumes isotropy and perfect bonding | Kerner, J. Mech. Phys. Solids, 1956 |
| Halpin–Tsai | Fibers / Platelets | Ec=Em(1+ξηϕ1−ηϕ)E_c = E_m \left( \frac{1 + \xi \eta \phi}{1 - \eta \phi} \right) | Short fibers, nanotubes, clay, graphene | Semi-empirical; accuracy depends on aspect ratio ξ\xi | Halpin & Kardos, Polym. Eng. Sci., 1976 |
| Nielsen–Lewis | Platelets | Ec=Em(1+Aϕ1−Bϕ)E_c = E_m \left( \frac{1 + A\phi}{1 - B\phi} \right) | Platelets (nanoclay, mica), barrier materials | Requires calibrated constants A and B | Nielsen, J. Macromol. Sci., 1967 |
| Tandon–Weng | Short Fibers | Analytical (complex) | Randomly or partially aligned short fibers | Assumes uniform orientation distribution | Tandon & Weng, Composites Sci. Technol., 1984 |
| Mori–Tanaka | Ellipsoidal (fibers, rods) | Numerical/matrix-based | General high-aspect fillers with interaction effects | Complex; assumes perfect interface and uniformity | Mori & Tanaka, Acta Metall., 1973 |
| Voigt (Rule of Mixtures – Upper Bound) | Any | Ec=ϕEf+(1−ϕ)EmE_c = \phi E_f + (1 - \phi) E_m | Aligned long fibers | Overestimates for non-aligned systems | Voigt, 1889 |
| Reuss (Lower Bound) | Any | 1Ec=ϕEf+1−ϕEm\frac{1}{E_c} = \frac{\phi}{E_f} + \frac{1 - \phi}{E_m} | Load perpendicular to fiber direction | Underestimates actual behavior | Reuss, 1929 |
| Hashin–Shtrikman Bounds | Any shape | Bound equations | Theoretical limits for isotropic composites | Not predictive, just bounding | Hashin & Shtrikman, J. Mech. Phys. Solids, 1963 |

Halpin-Tsai Model

| Optimizer | Sigma | FM | Cerr 117 | Cerr 158 | Average |
| --- | --- | --- | --- | --- | --- |
| FM | 20.2403 | 9.58 | 14.94 | 18.01 | 14.18 |
| Cerr 117 | 17.4941 | 10.02 | 11.42 | 14.11 | 11.85 |
| Cerr 158 | 16.8656 | 10.61 | 12.25 | 13.22 | 12.03 |
| Averaged | 18.2 | 9.9 | 11.96 | 15.11 | 12.32 |
| All materials combined | 17.49 | 10 | 11.4 | 14.11 | 11.9 |
| Buckner et al* | 8.51 | 34.7 | 33.72 | 29.48 | 32.63 |

*with true averaged aspect ratio

Assumption: Young’s modulus of the material assumed to be similar to the modulus of the FM 9.25GPa.

Final selection 17.5 as sigma

Final selection

Guth A=3  B=0.3

Tsai Sigma = 17.5

| Model | Average % Improvement |
| --- | --- |

| Guth | 47.82% |
| --- | --- |

| Tsai | 63.66% |
| --- | --- |

Assu

Considering the analysis; Guth model has been selected considering the less error.

Kruskal-wallis test has been used to identify the

Concentration 10%:

p-value = 0.3679

➤ No significant difference between materials

Optimization for A and B

| Optimizer | A | B | FM | Cerr 117 | Cerr 158 | Average |
| --- | --- | --- | --- | --- | --- | --- |
| FM | 0.99 | 0.01 | 9.75 | 13.39 | 16.5 | 13.21 |
| Cerr 117 | 0.89 | 0.11 | 10.02 | 11.42 | 14.1 | 11.85 |
| Cerr 158 | 0.86 | 0.14 | 10.6 | 12.25 | 13.22 | 12.02 |
| Buckner et al | 0.375 | 0.625 | 34.7 | 33.72 | 29.48 | 32.63 |